## Slide 1
Single-Component Order Parameter in URu2Si2 Uncovered by Resonant Ultrasound Spectroscopy and Machine Learning (arXiv: 1903.00552)
Michael Matty1, Sayak Ghosh1, Ryan Baumbach2, Eric D. Bauer3, K.A. Modic4, Arkady Shekhter2, J.A. Mydosh5, Eun-Ah Kim1 and B.J. Ramshaw1
1Department of Physics, Cornell University, USA; 2National High Magnetic Field Laboratory, USA; 3Los Alamos National Laboratory, USA; 4Max-Planck-Institute for Chemical Physics of Solids, Germany; 5Leiden University, The Netherlands
Elastic moduli jumps related to OP Dimensionality
Abstract
Resonant Ultrasound Spectroscopy Experiments
Add your information, graphs and images to this section.
Machine Learning can classify OP dimensionality
Fig. 3: Irreps of strain in URu2Si2 and
examples of singlet and doublet OP’s
Doublet
Singlet
Fig. 2: RUS setup and spectrum
Fig. 4: Irrep tensor product table for tetragonal group D4h
Fig. 6: Temperature evolution of URu2Si2 elastic moduli
Fig. 5: Temperature evolution of representative resonances
Solving elastic equation for larger sample suggests singlet OP
ANN finds single component OP for both samples
Fig. 7: Training data generation and artificial neural network
Fig. 8: ANN analysis for two samples of URu2Si2, (a) S1 and (b) S2
Fig. 1: Phase Diagram of URu2Si2
Strain εk couples to OP η → discontinuity in modulus
For HO transition, lowest order coupling is η2εk
A1g, A2g, B1g, B2g → Singlet, Eg → Doublet
Elastic moduli jumps classify OP dimensionality because OP bilinears couple to different moduli
Calculate elastic moduli through THO
Jumps in two A1g moduli, no jumps in shear moduli
Thermodynamic evidence for singlet OP
RUS measures mechanical resonances of a single crystal
Measures full elastic tensor simultaneously
At each resonance, strain field decomposes in terms of irreps of URu2Si2 point group
Larger URU2Si2 samples are lower quality
Traditional analysis fails for smaller samples:
  Missing resonances
  Ill defined sample geometry
We know that OP symmetry affects typical jump size
Design ANN to classify RUS spectra by OP dimensionality, even with missing peaks and ill defined sample geometry!
S2 has higher THO than S1 → higher quality
Singlet confidence from ANN peaks near experimental THO
ANN classifies the OP as singlet for both samples!
(a)
(b)
Conclusions, outlook, and acknowledgements
Both analyses support singlet OP
Result independent of microscopic mechanism
Can extend RUS to materials where large single crystals unavailable
ML framework transferable to other spectroscopic techniques like NMR
Figure 1 from Kasahara et al., New J. Phys., 11, 055061 (2009)
Figs. 2,3,5-8 from Ghosh, Matty et al., arXiv:1903.00552 (2019).
The superconductivity in URu2Si2 condenses from an unusual correlated state called ‘Hidden Order’, which onsets at THO=17.5 K. The order parameter(OP) characterizing this state has stayed ‘hidden’ for over 30 years. We use resonant ultrasound spectroscopy(RUS), coupled with a novel machine learning based analysis technique, to constrain the order parameter to be single-component(singlet).
The framework we have developed should be readily applicable to other correlated states of matter, such as the pseudogap in cuprates, and the superconductivity of Sr2RuO4